Preparation and Characterisation of Nanostructured Metal Films
Speaker: Sam Moore
Supervisors: Sergey Samarin, Jim Williams
Centre for Atomic Molecular and Surface Physics

---
Introduction
- Nanostructured thin films have been studied for more than a century due to their interesting optical properties
  - Faraday, 1857 – Bakerian Lecture
- Many of these properties can now be understood in terms of the behaviour of conduction and valence band electrons
- 1908: G. Mie – Theory for scattering of light by spherical particles; Gold colloids in stained glass
Source:
http://traumwerk.stanford.edu/philolog/2006/01/abbe_sugers_theory_of_light_lu.html
[Speaker Notes: Medieval Stained Glass An example of interesting optical effects in thin films of gold nanoparticles Investigated by Mie in 1908 Different colours obtained by different sizes of gold nanoparticles Mie Theory for light scattering from spherical nanoparticles; still widely used today]

---
Modern Interest in Nanostructured films: Plasmonics
- Plasmon = Collective (conduction) electron density oscillations
- 1957: Ritchie - Surface plasmons occur near the surface of metallic structures
- The structure of the surface is crucial in determining the behaviour of plasmons
  - Propagating or Localised (in metal nanoparticles)
  - Coupling of photon and plasmon - Polariton

---
A “Blackened” Plasmonic meta-material
P-polarised
S-polarised
x
y
Sondergaard et al. Plasmonic black gold by adiabatic nanofocusing
and absorption of light in ultra-sharp convex
Grooves, Nature Communications, July 2012
[Speaker Notes: Very recent development (June 2012)]

---
Black Metal Films
- A technologically simple nanostructured film with many optical applications
- Deposition of noble metals at high pressure
- Originally discovered in 1930s (Pfund)
  - Near perfect black body; low thermal mass
- Applications:
  - Radiometric devices
  - Infra-red detectors
  - Thin film solar cells

---
This project
- Aim: Prepare and characterise both Black and non-black nanostructured metal films
- Techniques:
  - Scanning Electron Microscopy
  - Total Current Spectroscopy
  - Optical Spectroscopy
  - Spectroscopic Ellipsometry

---
Sample Preparation & Vacuum Chamber Setup

---
SEM Images of Prepared Samples
“Bright” Au (3.5A 5min 1e-6mbar)
“Black” Au (3.5A 5min 0.18mbar)
200nm
Credit: Centre for Microscopy Characterisation and Analysis (CMCA) UWA
[Speaker Notes: SEM Image of a Au film Deposited in He at 1e-6 mbar Regular array of metal nanoparticles (Sizes 20nm to 100nm)]

---
Total Current Spectroscopy
1. Simplified Schematic
3. Block Diagram
2. Electron gun
[Speaker Notes: I1 = Incident current of electrons (constant) I2 = Scattered (inelastic & elastic) electrons I = Final curent of electrons (Measured) U = Applied potential between cathode and sample; determins energy of electrons E = eU + C]

---
Contact Potential
Electrons emitted with distribution in energies
No current measured unless applied potential > contact potential
Potential of a real surface is not actually a step function

---
General shape of TCS curves
Total Current Spectrum = Derivative of measured current
Signal modulation at threshold energies for elastic/quasielastic and inelastic processes
Elastic peak when energy of primary electrons overcomes the contact potential
Thresholds for inelastic processes show up at higher U
Potential of surfaces are not step functions
May see additional elastic peaks, particularly for non-uniform surfaces
Elastic scattering peaks are convolved with inelastic scattering

---
Tuning the Electron Gun
Electron gun determines effective energy distribution of primary electrons at target
Manually find optimum electrode potentials by iterative trial and error process
1. Focusing on Au (bright) on Si
2. Simplified simulations of gun
[Speaker Notes: TCS is a secondary electron spectroscopic technique which is sensitive to behaviour of electrons near a surface Elastic scattering (due to potential seen by primaries) – major part of signal Inelastic scattering (interband transitions, plasmon excitations) Advantage: Simple to realise; does not resolve energies of secondary electrons Integration into vacuum chamber allows almost immediate study of samples]

---
Deposition of Ag on Si
Literature Work Functions:
Si:	4.6 – 4.9eV
Ag:	4.2 – 4.7eV
SiO2:	5.0 – 6.0eV

---
Deposition of Black Ag on the Ag on Si

---
Variable Angle Spectroscopic Ellipsometry
1. Ellipsometric measurement
Source: 1. T.W.H. Oates et al, Characterization of plasmonic effects in thin films and
metamaterials using spectroscopic ellipsometry, Progress in Surface Science, 2011
[Speaker Notes: Measures the change in polarisation of light reflected from a sample Can relate directly to optical constants of sample Direct detection of surface plasmons: Change in reflectivity of s vs p polarised light Indirect: determination of possible plasmon frequencies through the pseudo-dielectric constant]

---
Ellipsometer Modelling Procedure
Source: J.A. Woolam et al, Overview of Variable Angle Spectroscopic Ellipsometry (VASE), Part I: Basic Theory and Typical Applications, Optical Metrology 1999

---
Comparison of Black Ag and Ag thin films on Si
Black Ag on Si Model
(MSE = 46.45)
Ag on Si Model
(MSE = 2.99)
EMA (fit 76% void) 3.41nm
Ag (fit n&k)	6.96nm
SiO2	3.11nm
Si	(substrate)
EMA (50% void) 1.02nm
Ag (fit n&k)	16.09nm
Intermix (SiO2)	0.27nm
SiO2	4.02nm
Si	(substrate)

---
Comparison of Black Ag and Ag thin films on Si
Ag on Si Model
(MSE = 2.99)
Black Ag on Si Model
(MSE = 46.45)
EMA (50% void) 1.02nm
Ag (fit n&k)	16.09nm
Intermix (SiO2)	0.27nm
SiO2	4.02nm
Si	(substrate)
EMA (fit 76% void) 3.41nm
Ag (fit n&k)	6.96nm
SiO2	3.11nm
Si	(substrate)

---
Conclusions
Prepared a range of metallic nanostructured films under different conditions
  - Preparation pressure determines optical properties of film
SEM images show structural differences between Black and Bright Au films
  - Bright Au: Regular, roughly spherical nanoparticles
  - Black Au: Randomised, porous structures
TCS demonstrates change in elastic scattering with film deposition
  - Lowering of contact potential when Ag deposited on Si
  - Deposition of Black Ag on the existing Ag on Si: Narrowing of elastic peak
  - Possible Application of TCS: Monitor the deposition of metallic films
Optical constants of Black Ag and Bright Ag thin films differ significantly
  - Ag differs from bulk, but qualitatively similar
  - Black Ag model shows large peaks in both n and k near 370nm

---
Accuracy of model for Ellipsometric Data
Ag: MSE = 2.99

---
Accuracy of model for Ellipsometric Data
Black Ag: MSE = 46.56

---
Accuracy of model for Ellipsometric Data
Black Ag: MSE = 46.56

---
Considerations for Modeling Films
Fit may not converge to global minima; need to have good initial values
Source: J. A Woolam WVASE32 Manual

---
Use of Electron gun simulations
Qualitative only; understand behaviour of gun

---
Use of Electron gun simulations
Qualitative only; understand behaviour of gun
Insulating posts are here!!!

---
Error/Processing of TCS
Pole as h -> 0
Smoothing reduces noise and fine structure

---
Error/Processing of TCS
MSE for smoothed curve:

---
Full circuit for TCS

---
Block Diagram for TCS

---
Error in Ellipsometric Measurements
Black Ag n & k peaks

---
Transmission Spectra of Black Au

---
Applications of Black Metal Films
- Applications:
  - 1930s: Radiometric devices (Pfund)
  - 1950s: Infra-red detectors (Harris et. al)
    - Later: Pyro-detectors
  - 2010s: Thin film solar cells (Panjwani)
    - Possible plasmonic resonance effects
Image Source: http://en.wikipedia.org/wiki/File:Crookes_radiometer.jpg

---
Peak in k – Link to plasmonics
Peaks in Extinction coefficient have been linked to plasmons
Source: Yue Bing Zheng, and Tony Jun Huang, Surface plasmons of Metal Nanostructure Arrays:
From Nanoengineering to Active Plasmonics